Sample Stormdrain Specification for Design Engineers #1

Counties that allow 16 Gauge CMP

Stormdrain pipe shall be any of the following:

- Spiral rib corrugated steel pipe per AASHTO M36 and ASTM A760 with a Manning’s coefficient of 0.012. Coating shall by aluminized type 2 per AASHTO M274 and ASTM A929. Pipe diameters 12” thru 36” shall be 16 gauge minimum, 42” thru 48” shall be 14 gauge minimum, 54” thru 84” shall be 12 gauge minimum. Pipe to be installed per the requirements of ASTM A798 and AASHTO Section 26.

- High Density Polyethylene (HDPE) pipe per the requirements of AASHTO M294 Type S and AASHTO M252 type S (smooth interior, corrugated exterior). Pipe to be installed per the requirements of ASTM D2321 and AASHTO Section 30. ASTM F2648 pipe is not an acceptable substitution.

- Reinforced Concrete Pipe per the requirements of ASTM C76. Pipe shall be class 3 minimum. Pipe shall be installed per the requirements of ASTM C1479 and AASHTO Section 27.

Note: Where this specification disagrees with municipal ordinance, municipal ordinance shall prevail.

Sample Stormdrain Specification for Design Engineers #2

Counties with a 14 Gauge CMP requirement

Stormdrain pipe shall be any of the following:

- Spiral rib corrugated steel pipe per AASHTO M36 and ASTM A760 with a Manning’s coefficient of 0.012. Coating shall by aluminized type 2 per AASHTO M274 and ASTM A929. Pipe diameters 12” thru 48” shall be 14 gauge minimum, 54” thru 84” shall be 12 gauge minimum. Pipe to be installed per the requirements of ASTM A798 and AASHTO Section 26.

- High Density Polyethylene (HDPE) pipe per the requirements of AASHTO M294 Type S and AASHTO M252 type S (smooth interior, corrugated exterior). Pipe to be installed per the requirements of ASTM D2321 and AASHTO Section 30. ASTM F2648 pipe is not an acceptable substitution.

- Reinforced Concrete Pipe per the requirements of ASTM C76. Pipe shall be class 3 minimum. Pipe shall be installed per the requirements of ASTM C1479 and AASHTO Section 27.

Note: Where this specification disagrees with municipal ordinance, municipal ordinance shall prevail.